## Slide 1
Low Volume Road Solutions
By: Jason Panter
Notes: Hi I’m Chris Dechkoff from ACP Applied products
The title of my presentation is Low Volume Road Solutions

## Slide 2
Seal Coats
What is a Seal Coat?
  Thin surface treatments
  Binder & Aggregates
Notes: So what does it mean to have a seal coat?
A collective term for several different kinds of thin surface treatments.
Applications of asphalt material that is usually covered with aggregates.

## Slide 3
Seal Coats
Why are Seal Coats Used?
    Protect structure
    Improve texture
    Correct non-structural deficiencies
        Aged or oxidized pavement
        Cracking
        Raveling
        Lack of skid resistance
    Wearing Course
    Dust Control
Notes: Why are Seal Coats used and what benefit do they have?
Used to protect pavement or substructure from water infiltration
Improve surface texture (increase skid resistance)
To correct non-structural deficiencies
    Aged or oxidized pavement
    Cracking
    Raveling
    Lack of skid resistance
Provide a wearing course over a base or porous product
Works well as dust control while providing a solid wearing course

## Slide 4
Gravel Seals
High Float asphalt emulsion
Unwashed graded aggregate (gravel).
Wearing and water-proofing course.
Applied to a variety of surfaces:
    Sub-grade
    Base
    Pavement
    Stabilized Bases
Binder
Graded-aggregate
Unprimed substrate
Notes: An application of High Float asphalt emulsion followed by an application of unwashed graded aggregate.
Primarily used as a wearing and water-proofing course.
Can be applied to a variety of surfaces:
    Sub-grade
    Base
    Pavement
    Stabilized bases

## Slide 5
Gravel Seals
Compacted Gravel Base
How to build one
    Emulsion layer sprayed first
    Aggregate layer evenly distributed
    Packed for orientation
    Repeat
Notes: So how does one go about building a gravel seal? Either a single or a double seal.
The concept of gravel seal is as illustrated on this slide.
First off the gravel base or substrate that the seal is to be placed on must be compacted properly and shaped to the desired profile
Next the binder is placed onto the granular base or substrate then the aggregate (gravel) layer is distributed evenly
The placement process to this point is identical to conventional chip seals.
With rolling the low viscosity emulsion percolates into the aggregate matrix upwards and also downwards and helps orientation of the particles
Here you have a completed single gravel seal
This process is then repeated to construct a double gravel seal.

## Slide 6: Gravel Seals
Notes: Graded Seal Coat Application and Construction in Provost, Alberta

## Slide 7
Gravel Seals
Notes: Here is an example of a double gravel seal on a compacted gravel base after initial construction for the MD of Provost
The road surface is quite rough but with traffic and time the surface will knead together

## Slide 8: Fibermat Option
Direction of Application
Chippings
Chopped fibres
First layer of emulsion
Second layer of emulsion
Notes: This is a diagram that shows all the main element of the trailer unit including the space within the trailer for the storage of spools of fibre, the conduits that bring the stands of fibre to the chopping units and chamber.
The diagram also shows the two spray bars located in front and behind the fibre distribution unit.
Chippings are then applied on top of the fibre-reinforced membrane and embedded into the binder to form a fibre-reinforced surfacing or interlayer system.
The trailer unit contains sufficient fibre in storage for the placement of 40,000 m2 of fibre-reinforced membrane before re-loading. The width of placement can vary from 3.0 to 4.0 m.

## Slide 9: Fibre Option
First Application of binder
Application of Fibres
(60mm length at 75 g/m2)
Second Application of binder

## Slide 10: Fibermat Option
(Double Gravel Seal)
Notes: Fibermat can be utilized as an addition to most seal coat operations.
Here it can be seen being utilized in a double gravel seal on the initial application directly on the compacted gravel base for the MD of Provost
Fibermat can be used in multi-chip applications as well as single applications.

## Slide 11: Fibermat Option
Notes: Here is a quick video of the Fibermat operation.
As is evident in the video the operation does not slow down the application process of the binder and operates much like a traditional seal coat process.

## Slide 12
Fibermat Option
Notes: Here is an example of what a section of roadway looks like with the addition of Fibermat.
Upon initial investigation it looks like any other seal coated road.
It will not be until further years when maintenance of these roads is reduced that it will become evident that it possesses Fiber.

## Slide 13: Performance
Notes: Double GravelSeal Coat with Fibre
This is the first double gravel seals with fibre-reinforcement applied on a public roadway.
The work was carried out in 2011 in Macklin, Saskatchewan.

## Slide 14: Performance
Before
After
Notes: Double GravelSeal Coat with Fibre

## Slide 15: Performance
Before
After
Notes: Double Gravel Seal Coat with Fibre

## Slide 16: Performance
Aggregate Req’d: 600 MT/km
Type: 12.5C Gravel
Binder : HF150P

## Slide 17: Performance
Notes: This is also a double gravel seal with fibre-reinforcement.
The work was carried out in 2010 in the Northwest Territories near Yellowknife in 2010.
The picture shown here was taken only a few weeks ago.

## Slide 18: Ballpark Pricing
Single with Fiber (Supply) = $4.00 - $6.00
Single No Fiber (Supply) = $3.00 - $4.00
Single with Fiber (No Supply) = $3.00 - $5.00
Single No Fiber (No Supply) = $2.00 - $3.00
Double with Fiber (Supply) = $7.00 - $9.00
Double No Fiber (Supply) = $6.00 - $8.00
Double with Fiber (No Supply) = $6.00 - $8.00
Double No Fiber (No Supply) = $5.00 - $6.00

## Slide 19: Offering
Produce our own Emulsions
Aggregate Testing
Seal Coat and Cold Mix Designs
Construction
Solutions for your road networks

## Slide 20: Questions?
Chris Dechkoff, P.Eng.
cdechkoff@acpapplied.com
www.acpapplied.com